United Chemical&Textile

Sequestering agent LD-110

Sequestering agent LD-110 forms water-soluble complexes with the ions of alkaline earth and heavy metals. It is suitable for softening treatment baths, removing incrustations by water-hardening salts and preventing yellowing of the fabric caused by iron compounds.

[Properties]

- Appearance: colorless transparent liquid

- Chemical character: based on organic acids

- Ionicity: weak anionic

- PH value （1％ solution）: 6.0～7.0

- Solubility: can be mixed with water in any proportion

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- It ionizes metal particles thus avoiding catalytic damage to the cotton and destabilization of the peroxide bath.

- It demineralizes cotton and removes stubborn pigments.

- It is bioeliminable.

[Applications]

Discontinuous method:   0.5-1g/L  LD-110

Continuous method:     1-2g/L  LD-110

[Packaging]

Packed in Plastic Drums and 125kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.