United Chemical&Textile

Easy Care Finish Resin NCD

NCD is a crosslinking agent for the chlorine-fast ,easy-care finishing of textiles composed of cellulosic fibres and their blends with synthetic fibres. It gives lower fabric formaldehyde levels while maintaining high physical performance.

[Properties]

- Appearance: light yellow, transparent and low viscous liquid

- Chemical character: Modified N and N-hydroxymethyl dihydroxy ethylene urea

- pH value: 4.0-5.0

- Solubility: can be mixed with water in any proportion

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- Very good easy care effects that are resistant to washing at the boiling and dry cleaning.

- High resistance to hydrolysis .

- Good chlorine stability of finishes measured by the AATCC 92 test method.

[Applications]

Resin NCD is applied by padding at room temperature. The liquor pickup is 60-90%, depending on the types of goods.

Catalyst CS-200  is especially suitable.

Amounts used (based on quantity of resin NCD)

25-30% Catalyst CS-200

Examples of use

A) Used on woven fabric    100％ cotton

Resin NCD               60～100g/l

Catalyst CS-200           18～30g/l

Softener DT-5250           20～40g/l

softener DT-6500     　    20～30g/l

pad, dry and cure 3min at 150℃ (or cure 45s at 175℃)

B) Used on knitted fabrics      100％ cotton

Resin NCD                20～40g/l

Catalyst CS-200           15～20g/l

Softener DT-5250          15～20g/l

Softener DT-6500          20～30g/l

pad, dry and cure 3min at 150℃ (or cure 45s at 175℃)

[Packaging]

Packed in Plastic Drums and 140kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.