United Chemical&Textile

Easy Care Finish Resin NFD

NFD is a concentrated resin for easy-care finishing of textiles composed of cellulosic fibres and their blends with synthetic fibres. It gives extremely fabric formaldehyde levels while maintaining high physical performance.

[Properties]

- Appearance: light yellow, transparent and low viscous liquid

- Chemical character: Modified N and N-hydroxymethyl dihydroxy ethylene urea

- pH value: 4.0-5.0

- Solubility: can be mixed with water in any proportion

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- Resin NFD, in combination with catalyst CS-200 or catalyst CQ-200, produces particularly low formaldehyde finishing effects.

- When correctly applied Resin NFD, meets all the requirement of consumer labels such as Eco-Tex Standard 100 for textiles near to the skin（＜75ppm formaldehyde on the goods）

- High resistance to hydrolysis and low chlorine effect.

[Applications]

Resin NFD is applied by padding at room temperature. The liquor pickup is 60-90%, depending on the types of goods.

Catalyst CS-200 or CQ-200 is especially suitable.

Amounts used (based on quantity of resin NFD)

25-30% Catalyst CS-200

20-25% Catalyst CQ-200

Examples of use

A) Used on woven fabric      100％ cotton

Resin NFD              60～100g/l

Catalyst CS-200           18～30g/l

Softener DT-5250          20～40g/l

softener DT-6500     　   20～30g/l

pad, dry and cure 3min at 150℃ (or cure 45s at 175℃)

B) Used on knitted fabrics      100％ cotton

Resin NFD                20～40g/l

Catalyst CS-200           15～20g/l

Softener DT-5250          15～20g/l

Softener DT-6500          20～30g/l

pad, dry and cure 3min at 150℃ (or cure 45s at 175℃)

[Packaging]

Packed in Plastic Drums and 140kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.