United Chemical&Textile

Anionic Softener DT-3000

Softener DT-3000 is a high efficient anionic softener with hydrophilic properties for cellulosic fibre and their blends with synthetic fibres.

[Properties]

- Appearance: light yellow semi-solid paste

- Chemical character: carboxylic acid ester sulphonate

- Ionicity: anionic

- PH (1% aqueous solution):7.0-9.0

- Solubility: soluble in cold water

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features ]

- Produces Smooth, dry, silk-like softening effects;

- Makes the goods hydrophilic and imparts antistatic properties;

- Has very little influence on the thermal migration behavior of disperse dyes on polyester fibres;

- improves the yarn sewability, and reduces the generation of needle holes;

- Is applicable by all the usual padding, immersion and spraying processes.

[Applications]

Before use, softener DT-3000 should be diluted in hot water that weights 9 times of a part.

Discontinuous method:  1.0-3.0 % o.w.f.

Continuous method:  10- 50g/l

[Packaging]

Packed in Paper Bags and 25kgs Net Each

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.