United Chemical&Textile

Migration Inhibitor LAM-88

LAM-88 is a migration inhibitor for pad dyeing with vat dyes, reactive dyes and disperse dyes.

[ Properties]

- Appearance: colorless viscous liquid

- Chemical character: based on acrylate copolymer

- Ionicity: weak anionic

- 1% solution pH value: 7±0.5

- Solubility: can be mixed with water in any proportion.

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- Extremely effective antimigrant for pad dyeing of textiles. Produces a smooth and uniform dye appearance.

- Runs clean with no roller buildup.

[Applications]

Continuous method:

For T/C blended fabrics

10-30g/l  LAM-88.

X g/l     disperse dyes

For cotton fabrics

10-20g/l   LAM-88

X g/l     vat dyes

[Packaging]

Packed in Plastic Drums and 125kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.