United Chemical&Textile

Fixing Agent GD-80

Fixing agent GD-80 is a kind of formaldehyde-free textile auxiliary for improving wet fastness on cotton dyeing with reactive dyes or direct dyes.

[Properties]

- Appearance: clear yellow liquid

- Chemical character: Aqueous preparation of a polymeric, quaternary ammonium

- Ionicity: cation

- PH (1% aqueous solution):6.0-7.0

- Solubility: can be infinitely diluted by cold water

- Storage: Can be stored for one year when the product is enclosed in the proper container under the room temperature.

[Features]

- Excellent water severe, perspiration and hot pressing fastness and improved fastness to wash.

- No contamination of goods or environment with formaldehyde (Oeko-Label).

[Applications]

Discontinuous method:  0.5-1.0 % o.w.f.    20 min at 40°C pH 6–7

Continuous method:  5- 8g/l    pad, dry at 120℃

[Packaging]

Packed in Plastic Drums and 125kgs Net Each.

The information and recommendations presented here were compiled with the utmost care,but cannot be extended to cover every possible case.They are intended to serve as non-binding guidelines and must be adapted to the prevailing conditions.